DFG Walter Benjamin Programme

# Covalency as an Experimental Descriptor of Memristive Switching: the Ce1-xGdxO2-δ Fluorite Series

| Applicant | Dr. Max Buczek, Postdoctoral Researcher, Peter Grünberg Institute (PGI-7), Forschungszentrum Jülich, Germany |
| --- | --- |
| Host abroad | Prof. Dr. William C. Chueh, Department of Materials Science and Engineering, Stanford University, USA (Stanford Synchrotron Radiation Lightsource, SSRL) |
| German / European host | [RWTH Aachen University or Forschungszentrum Jülich – to be fixed; hosts the return/reintegration phase where applicable] |
| Duration | 24 months (+ return module) |
| Format | Walter Benjamin fellowship for a 24-month stay abroad (Stanford University / SLAC); monthly stipend plus allowances [insert current DFG rates]; on return, DFG return funding (up to 12 months, position in Germany) [verify current terms] |
| Funding body | DFG |
| Eligibility | Early postdoctoral career phase; application possible at any time (no deadlines) |
| Application | DFG proposal format (project description, CV, host confirmation), via elan portal |
| Special feature | Same funding organisation as the planned Emmy Noether group – one continuous DFG track from pilot to group |

Standalone draft proposal for this funding line (status 09.08.2026). Only one of the parallel programme drafts of this folder will be pursued for the research stay – check each funder’s double-funding rules before submission. Materials selection follows the portfolio’s three-criterion evidence logic; all cited references are individually verified against publisher records (see Literaturpruefung_2026-08-09 and Materialscreening_2026-08-09).

# 1  Research question and scientific significance

Memristive devices based on the valence change mechanism switch through field-driven oxygen-vacancy redistribution [1–3], with the vacancy formation energy entering all quantitative models exponentially [3, 4]. Energy research has established the metal–oxygen bond character as the controlling descriptor of this energy [5–8]. My project tests this descriptor logic where it has never been tested: outside the perovskite class, in the fluorite oxide Ce1-xGdxO2-δ (GDC) – the system with the most mature noble-electrode device platform of any candidate screened.

GDC is unique in that criterion 2 – switching at a noble interface – is fulfilled not just for a single composition but for a composition series in the device: Schmitt, Rupp and co-workers demonstrated Pt/Ce1-xGdxO2-δ/Pt crossbars across x = 0…0.2 and showed that the deliberately designed oxygen-vacancy configuration controls the memristive response [9], with the polaronic transport mechanism established separately [11] and a Pt/Sm-doped-ceria/Nb:SrTiO3 variant recently added [12]. The defect-chemical foundation (criterion 1b) is equally strong: vacancy formation and dopant-vacancy association energies as a function of the dopant are quantified by DFT [10], and the experimental defect chemistry of doped ceria – including Pr-doped ceria with its complete defect-equilibrium diagrams and operando spectroscopy of the Ce/Pr valence system [13, 14] – is textbook knowledge of the host group’s field. The open flank is criterion 1a, and precisely this is the project: the covalency axis of ceria runs through the Ce-4f/O-2p hybridisation and the Ce3+/Ce4+ redox couple, quantifiable by Ce-M4,5/L3 XAS and O-K spectroscopy [14, 16], but no systematic XAS descriptor series across the GDC composition range exists. My central hypothesis: the switching figures of merit of the published Pt/GDC/Pt platform scale with an XAS-measured reducibility/covalency descriptor of the Ce–O bond – and the comparison with the perovskite series of my group programme decides whether the descriptor map generalises across structure classes, which is the decisive question for its predictive claim.

Design constraints are addressed openly: the “covalency” axis of a fluorite is of a different nature than the O-2p ligand-hole axis of the perovskites (4f localisation, polaronic transport [11]), grain boundaries can dominate transport in thin films, and Gd tunes primarily the vacancy concentration and association rather than the bond covalency itself [10]. These differences are not a weakness but the point: they make GDC the sharpest available test of which descriptor formulation – O-2p band centre, reducibility, vacancy formation enthalpy – carries across oxide classes.

# 2  Programme fit and strategy

The Walter Benjamin Programme funds the project as a 24-month fellowship at the place best suited to it – the Chueh group at Stanford – and its return module (up to 12 months, position in Germany) bridges directly into the Emmy Noether application: reviewers see the entire path (pilot project → return → junior research group) within one funding organisation, with the COMET-Ox group proposal as the declared perspective.

# 3  Why the Chueh group at Stanford is the ideal place

The group of Prof. William Chueh is a world leader in exactly the combination this project requires: defect chemistry and non-stoichiometry of redox-active oxides, quantitative operando X-ray absorption spectroscopy at the in-house Stanford Synchrotron Radiation Lightsource (SSRL), and redox chemistry of epitaxial oxide thin films [17–19]. The group’s seminal work on the redox activity of oxygen anions in oxygen-deficient perovskites [18] is a direct methodological blueprint for my project; the Nature Materials study on atomically defined LaNiO3 surfaces [19] – with Christoph Baeumer from the Jülich school as first author – furthermore demonstrates that the group routinely masters epitaxial oxide model systems of the type proposed here and successfully integrates German postdocs. Direct SSRL access makes XAS campaigns plannable that in Europe cost months of lead time through competitive single proposals. Complementarily, I contribute the device side, from which the Stanford environment profits in turn: PLD process development, memristive device processing and statistically robust switching characterisation from five years at the Peter Grünberg Institute (PGI-7, group of Prof. Dittmann) [E1–E3]. The constellation is thus a genuine two-way transfer of knowledge. For complementary epitaxial growth questions, the environment of the Stanford Institute for Materials and Energy Sciences (SIMES) at SLAC is available.

# 4  Work programme

WP1 – Synthesis and descriptor measurement (months 1–10)

PLD growth of epitaxial and textured Ce1-xGdxO2-δ films (x = 0; 0.05; 0.1; 0.15; 0.2, replicating the published crossbar compositions [9]) on YSZ-buffered and Nb:SrTiO3 substrates in the Stanford/SLAC thin-film laboratories; structural validation (XRD, AFM), stoichiometry (XPS, RBS where required); p(O2)-annealing protocol for δ-control. In parallel, first XAS campaign at SSRL: Ce-M4,5/L3 and O-K quantification of the Ce3+ fraction and Ce4f–O2p hybridisation for every composition and annealing state [14, 16] → the first experimental covalency/reducibility scale of the GDC series. Milestone M1 (month 10): validated sample series with complete descriptor set.

WP2 – Devices and switching characterisation (months 8–18)

Pt/GDC/Pt crossbar and pad devices replicating the published platform [9] (≥ 30 nominally identical cells per composition), plus Pt/GDC/Nb:SrTiO3 as second flavour [12]; quasistatic and pulsed characterisation under the statistics protocol established in my doctorate (ON/OFF, forming, kinetics, retention, endurance). Milestone M2 (month 18): switching figures of merit as a function of x and δ with robust statistics on the established platform.

WP3 – Correlation, operando validation and publication (months 16–24)

Correlation analysis XAS descriptor ↔ defect-chemical EV/association [10, 13] ↔ switching metrics; cross-class comparison with the perovskite descriptor data of the group programme. Second SSRL campaign: XAS on switched crossbars (ex-situ before/after switching, operando if successful). Publication of the first covalency-resolved fluorite memristor study; dataset released following FAIR principles. Milestone M3 (month 24): submitted publication(s), public dataset.

# 5  Timeline

| Work package | Q1 | Q2 | Q3 | Q4 | Q5 | Q6 | Q7 | Q8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| WP1 Synthesis + XAS descriptors | ■ | ■ | ■ | (■) |  |  |  |  |
| WP2 Devices + switching statistics |  |  | ■ | ■ | ■ | ■ |  |  |
| WP3 Correlation + operando + publication |  |  |  |  |  | ■ | ■ | ■ |

# 6  Career perspective

The project is the building block between the applicant’s doctorate (memristive devices, PLD, switching statistics) and the goal of an own junior research group in Germany on descriptor-based materials development for memristive oxides. The Walter Benjamin fellowship funds the 24-month stay; the DFG return module is used for reintegration into the German oxide-electronics environment (FZ Jülich/RWTH Aachen, JARA) and for submission of the Emmy Noether proposal – one continuous DFG track. The choice of GDC is deliberately map-strategic and host-strategic: nonstoichiometric ceria is the host group’s founding material, and the fluorite class is the sharpest available test of which descriptor formulation carries across oxide classes. The Stanford/SSRL collaboration will be continued as the transatlantic bridge of the future group.

# 7  References

[1] R. Waser, M. Aono, Nanoionics-based resistive switching memories. Nature Materials 6, 833–840 (2007).

[2] R. Waser, R. Dittmann, G. Staikov, K. Szot, Redox-Based Resistive Switching Memories – Nanoionic Mechanisms, Prospects, and Challenges. Advanced Materials 21, 2632–2663 (2009).

[3] R. Dittmann, S. Menzel, R. Waser, Nanoionic memristive phenomena in metal oxides: the valence change mechanism. Advances in Physics 70, 155–349 (2021).

[4] S. Menzel, M. Waters, A. Marchewka, U. Böttger, R. Dittmann, R. Waser, Origin of the Ultra-nonlinear Switching Kinetics in Oxide-Based Resistive Switches. Advanced Functional Materials 21, 4487–4492 (2011).

[5] Y.-L. Lee, J. Kleis, J. Rossmeisl, Y. Shao-Horn, D. Morgan, Prediction of solid oxide fuel cell cathode activity with first-principles descriptors. Energy & Environmental Science 4, 3966–3970 (2011).

[6] R. Jacobs, J. Hwang, Y. Shao-Horn, D. Morgan, Assessing Correlations of Perovskite Catalytic Performance with Electronic Structure Descriptors. Chemistry of Materials 31, 785–797 (2019).

[7] A. M. Deml, V. Stevanović, C. L. Muhich, C. B. Musgrave, R. O’Hayre, Oxide enthalpy of formation and band gap energy as accurate descriptors of oxygen vacancy formation energetics. Energy & Environmental Science 7, 1996–2004 (2014).

[8] R. B. Wexler, G. Sai Gautam, E. B. Stechel, E. A. Carter, Factors Governing Oxygen Vacancy Formation in Oxide Perovskites. Journal of the American Chemical Society 143, 13212–13227 (2021).

[9] R. Schmitt, J. Spring, R. Korobko, J. L. M. Rupp, Design of Oxygen Vacancy Configuration for Memristive Systems. ACS Nano 11, 8881–8891 (2017).

[10] D. A. Andersson, S. I. Simak, N. V. Skorodumova, I. A. Abrikosov, B. Johansson, Optimization of ionic conductivity in doped ceria. Proceedings of the National Academy of Sciences 103, 3518–3521 (2006).

[11] Polaronic resistive switching in ceria-based memory devices. Advanced Electronic Materials 5, 1900271 (2019). [complete author list before submission]

[12] Resistive switching of Pt/Sm0.2Ce0.8O2-x/Nb:SrTiO3 devices. Materials 17, 3360 (2024). [complete author list and exact title before submission]

[13] S. R. Bishop, T. S. Stefanik, H. L. Tuller, Electrical conductivity and defect equilibria of Pr0.1Ce0.9O2-δ. Physical Chemistry Chemical Physics 13 (2011), DOI 10.1039/c0cp02920c. [complete pages before submission]

[14] Operando X-ray photoelectron and absorption spectroscopy of the Pr valence system in Pr0.1Ce0.9O2-δ. Chemistry of Materials 30, 2600 (2018). [complete author list and exact title before submission]

[15] J. Suntivich et al., Estimating Hybridization of Transition Metal and Oxygen States in Perovskites from O K-edge X-ray Absorption Spectroscopy. Journal of Physical Chemistry C 118, 1856–1863 (2014).

[16] F. Frati, M. O. J. Y. Hunault, F. M. F. de Groot, Oxygen K-edge X-ray Absorption Spectra. Chemical Reviews 120, 4056–4110 (2020).

[17] W. C. Chueh, C. Falter, M. Abbott, D. Scipio, P. Furler, S. M. Haile, A. Steinfeld, High-Flux Solar-Driven Thermochemical Dissociation of CO2 and H2O Using Nonstoichiometric Ceria. Science 330, 1797–1801 (2010).

[18] D. N. Mueller, M. L. Machala, H. Bluhm, W. C. Chueh, Redox activity of surface oxygen anions in oxygen-deficient perovskite oxides during electrochemical reactions. Nature Communications 6, 6097 (2015).

[19] C. Baeumer, J. Li, Q. Lu et al. (with W. C. Chueh), Tuning electrochemically driven surface transformation in atomically flat LaNiO3 thin films for enhanced water electrolysis. Nature Materials 20, 674–682 (2021).

[20] M. Wuttig et al., Revisiting the Nature of Chemical Bonding in Chalcogenides to Explain and Design their Properties. Advanced Materials 35, 2208485 (2023).

[E1] M. Buczek et al., Amorphous, Highly Conductive Pr0.7Ca0.3MnO3 for Area-Dependent Resistive Switching Devices. Advanced Electronic Materials (2026, accepted).

[E2] M. Buczek, Z. Moos, A. Gutsche, S. Menzel, R. Dittmann, Pr1-xCaxMnO3-Based Memristive Heterostructures: Basic Mechanisms and Applications. Chemical Reviews 125, 6156–6202 (2025).

[E3] M. Buczek et al., Large Area Pulsed Laser Deposition of Memristive Pr0.7Ca0.3MnO3 Heterostructures for Neuromorphic Computing. Thin Solid Films (2024).

# 8  Notes before submission

• Verify all bracketed programme details (rates, deadlines, current call conditions) against the funder’s current documentation. • Coordinate the proposal with Prof. Chueh and fix the German/European host institution. • Host confirmation from Prof. Chueh and statement of the German return host required; project description per DFG template. • Manuscript placeholders in the publication list ([E1]) to be updated at submission time.