Alexander von Humboldt Foundation – Feodor Lynen Research Fellowship for Postdoctoral Researchers

Application for a Feodor Lynen Research Fellowship

Covalency as an Experimental Descriptor of Intrinsic Memristive Switching: the SrTi1-xFexO3-δ Model Series

| Applicant | Dr. Max Buczek, Postdoctoral Researcher, Peter Grünberg Institute (PGI-7), Forschungszentrum Jülich, Germany |
| --- | --- |
| Host | Prof. Dr. William C. Chueh, Department of Materials Science and Engineering, Stanford University, USA – Friedrich Wilhelm Bessel Research Award winner of the AvH Foundation (2021), member of the Humboldt Network |
| Host institution | Stanford University / SLAC National Accelerator Laboratory (Stanford Synchrotron Radiation Lightsource, SSRL) |
| Duration | 24 months, starting [e.g. Q2/2027; fellowship must begin 2–12 months after the selection meeting] |
| Programme line | Postdoctoral researchers (doctorate 2026, i.e. within the four-year window) |
| Targeted selection round | [February/June/October; submission recommended 4–7 months in advance] |

Note: This document contains the research proposal (exposé, max. 5 pages according to AvH requirements) and a checklist of the further application documents. The project is the 24-month nucleus, tailored to a research stay abroad, of the applicant’s longer-term research programme (Emmy Noether/ERC perspective after returning to Germany); per AvH requirements, the exposé must be coordinated with the host before submission.

# Research Proposal (Exposé)

## 1  Research question and scientific significance

Memristive devices based on the valence change mechanism (VCM) switch their resistance through field-driven creation and migration of oxygen vacancies (VO) [1–3]. The oxygen-vacancy formation energy (EV) enters all quantitative switching models exponentially [3, 4] – and yet it has never been measured systematically how EV determines the central figures of merit (ON/OFF ratio, forming voltage, retention). Energy research, by contrast, has quantitatively established that EV in perovskites is controlled by the metal–oxygen covalency: the O-2p band centre scales linearly with EV and serves as a descriptor for catalysis and oxygen transport [5–8]. My project connects these two worlds experimentally for the first time – using the model system SrTi1-xFexO3-δ (STF), the one perovskite series in which intrinsic switching, an inert/graphene electrode platform and a quantitatively mapped defect chemistry already coexist. A decisive design requirement drives this choice: in many perovskite memristors – including Pr0.7Ca0.3MnO3, the system of my own doctorate – robust switching requires a reactive metal electrode, and the oxygen exchange with the resulting second oxide (TiOx, AlOx) then dominates the mechanism [23, 24]. A clean covalency study must instead use a system whose oxygen balance stays inside the oxide.

STF is the ideal test system for a clean covalency study, for three reasons. (i) The covalency/reducibility axis is quantitatively mapped: STF forms a continuous cubic solid solution between SrTiO3 and SrFeO3-δ, and its defect chemistry is known in closed form – band gap Eg(x) = 3.2 − 1.9x + 0.5x² eV and reduction enthalpy ΔHred(x) = 5.8 − 3.4x + 1.7x² eV [9]; the Fe–O hybridisation across the series is documented by X-ray absorption [10–12]. The Fe content thus tunes the ease of oxygen-vacancy formation continuously within one perovskite host – the descriptor axis of this project, with literature values to test against. (ii) The switching axis is intrinsic – no reactive electrode required: Fe-doped SrTiO3 devices with inert electrodes switch via oxygen-vacancy modulation of the Schottky barrier (“eightwise”) as well as via intrinsic filaments [13, 14, 30]; Cr-doped SrTiO3 switches with inert electrodes with operando-XAS-proven vacancy drift [15]; and spectromicroscopy has traced the mechanism to oxygen migration and Ti valence changes within the oxide itself [16]. Crucially, the photoelectron-transparent graphene top-electrode platform has been demonstrated on exactly this materials system [17, 18]. Graphene is not merely convenient here but scientifically necessary: 18O-tracer and humidity studies show that under permeable electrodes, eightwise switching exchanges oxygen with ambient water [19, 20] – only a gas-tight (graphene-sealed) electrode makes the oxygen balance truly internal and the covalency–switching correlation unambiguous. (iii) The mechanism is stable across the series: for x ≤ 0.3, STF remains a cubic, p-type semiconducting perovskite – no topotactic brownmillerite transition and no metal–insulator transition interferes [9], in deliberate contrast to the manganite, ferrite and cobaltite families. The gap: a systematic Fe-content series in epitaxial devices under inert/graphene electrodes does not exist – published composition series were measured either with reactive electrodes (Ti/Pr1-xCaxMnO3 [23], where the electrode oxide dominates the mechanism [24]) or on polycrystalline films in a narrow composition window [22, 31]. My central hypothesis: the switching figures of merit of intrinsic STF devices scale with the covalency/reduction-enthalpy descriptor, with an optimum of the usable window at intermediate x – and the descriptor is measured, not merely computed [11].

## 2  Why the Chueh group at Stanford is the ideal place

The group of Prof. William Chueh is a world leader in exactly the combination this project requires: defect chemistry and non-stoichiometry of redox-active oxides, quantitative operando X-ray absorption spectroscopy at the in-house Stanford Synchrotron Radiation Lightsource (SSRL), and redox chemistry of epitaxial perovskite thin films [25–27] – STF itself is a canonical solid-oxide-fuel-cell and oxygen-permeation material, so its defect thermodynamics [9] lie squarely in the group’s home territory. The group’s seminal work on the redox activity of oxygen anions in oxygen-deficient perovskites [26] is a direct methodological blueprint for my project; the Nature Materials study on atomically defined LaNiO3 surfaces [27] – with Christoph Baeumer from the Jülich school as first author – furthermore demonstrates that the group routinely masters epitaxial perovskite model systems of the type proposed here and successfully integrates German postdocs. Direct SSRL access makes XAS campaigns plannable that in Europe cost months of lead time through competitive single proposals. Complementarily, I contribute the device side, from which the Stanford environment profits in turn: PLD process development, memristive device processing and statistically robust switching characterisation from five years at the Peter Grünberg Institute (PGI-7, group of Prof. Dittmann) [E1–E3] – the very school that established both the Fe:SrTiO3 switching platform and the graphene-electrode spectroscopy concept [13, 16–18], whose processing and metrology I know first-hand. This two-sided fit is the strongest possible de-risking for a 24-month project: the device platform is proven Jülich methodology, the defect-chemistry and XAS side is proven Stanford methodology, and the fellowship time is spent on their genuinely new combination. The constellation is thus a genuine two-way transfer of knowledge. For complementary epitaxial growth questions, the environment of the Stanford Institute for Materials and Energy Sciences (SIMES) at SLAC is available. As a Bessel Research Award winner (2021), Prof. Chueh is a member of the Humboldt Network and has repeatedly hosted German postdocs – the host eligibility required by the programme is given.

## 3  Work programme (24 months)

### WP1 – Synthesis and descriptor measurement of the STF series (months 1–10)

PLD growth of epitaxial SrTi1-xFexO3-δ films (x = 0; 0.02; 0.05; 0.1; 0.2; 0.3 – from the dilute-dopant regime of the established Fe:SrTiO3 devices [13] into the mixed-conducting regime, safely below the vacancy-ordering region) on Nb:SrTiO3 substrates in the Stanford/SLAC thin-film laboratories; structural validation (XRD, AFM); cation and oxygen stoichiometry (XPS, RBS where required). In parallel, first XAS campaign at SSRL: Fe-L2,3 and Ti-L2,3 valence analysis and O-K pre-edge quantification following [11] for every composition → experimental covalency scale of the series, benchmarked against the closed-form defect model [9] and the published STF spectroscopy [10]. Milestone M1 (month 10): validated sample series with complete descriptor set.

### WP2 – Intrinsic devices and switching characterisation (months 8–18)

Two inert top-electrode flavours per composition, processed photolithographically with ≥ 30 nominally identical cells each: (i) Pt pads as the workhorse geometry, and (ii) graphene-sealed cells – photoelectron-transparent and gas-tight, following the platform demonstrated on SrTiO3 [17, 18] – which keep the oxygen balance strictly internal [19, 20] and remain spectroscopy-ready. Interface control against unintentional layers follows the lessons of [21] (epitaxial platform, reference samples). Quasistatic and pulsed characterisation of the eightwise regime [13, 14, 29] under the statistics protocol established in my doctorate (ON/OFF at defined read-out voltage, forming requirement, kinetics, temperature-accelerated retention, endurance). Milestone M2 (month 18): switching figures of merit as a function of x, in both geometries, with robust statistics.

### WP3 – Correlation, operando validation and publication (months 16–24)

Correlation analysis covalency (XAS) ↔ ΔHred/EV (defect model [9], descriptor models [5–8]) ↔ switching metrics; test of the optimum hypothesis. Second SSRL campaign: XAS through the graphene electrode on switched cells (ex-situ before/after switching, operando if successful, following [17]) to verify that the composition-dependent differences rest on different VO dynamics inside the oxide. Publication of the first covalency-resolved study of intrinsically switching perovskite devices; dataset released following FAIR principles. Milestone M3 (month 24): submitted publication(s), public dataset.

## 4  Timeline

| Work package | Q1 | Q2 | Q3 | Q4 | Q5 | Q6 | Q7 | Q8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| WP1 Synthesis + XAS descriptors | ■ | ■ | ■ | (■) |  |  |  |  |
| WP2 Devices + switching statistics |  |  | ■ | ■ | ■ | ■ |  |  |
| WP3 Correlation + operando + publication |  |  |  |  |  | ■ | ■ | ■ |

## 5  Career perspective and return strategy

The project is the deliberate building block between my doctorate (memristive devices, PLD, switching statistics) and my longer-term goal of establishing my own junior research group in Germany on descriptor-based materials development for memristive oxides (Emmy Noether proposal in preparation; ERC Starting Grant as an alternative). The stay with Prof. Chueh closes the one competence gap of my profile – quantitative synchrotron XAS and defect thermodynamics – and at the same time delivers the empirical foundation (the covalency-resolved intrinsic STF dataset) for the larger programme of a “treasure map” of memristive oxides in analogy to the bonding-descriptor maps of Wuttig et al. [28]. The choice of STF for this fellowship is deliberate three times over: the switching stays inside the oxide (no reactive-electrode confounder), the graphene-sealed platform keeps it spectroscopy-ready and atmosphere-independent, and the mechanism is stable across the composition range. The subsequent group programme then scales the validated methodology to the mixed-valent A-site families (manganites, ferrites, cobaltites), where reactive interfaces and topotactic phase transitions are no longer confounders but become chartable mechanism boundaries on the map. The return is concretely planned: reintegration into the German oxide-electronics environment (FZ Jülich/RWTH Aachen, JARA), supported by the Feodor Lynen Return Fellowship, with submission of the group proposal during the final year of the stay. The Stanford/SSRL collaboration built up abroad will be continued as the transatlantic bridge of the future group.

## 6  References

[1] R. Waser, M. Aono, Nanoionics-based resistive switching memories. Nature Materials 6, 833–840 (2007).

[2] R. Waser, R. Dittmann, G. Staikov, K. Szot, Redox-Based Resistive Switching Memories – Nanoionic Mechanisms, Prospects, and Challenges. Advanced Materials 21, 2632–2663 (2009).

[3] R. Dittmann, S. Menzel, R. Waser, Nanoionic memristive phenomena in metal oxides: the valence change mechanism. Advances in Physics 70, 155–349 (2021).

[4] S. Menzel, M. Waters, A. Marchewka, U. Böttger, R. Dittmann, R. Waser, Origin of the Ultra-nonlinear Switching Kinetics in Oxide-Based Resistive Switches. Advanced Functional Materials 21, 4487–4492 (2011).

[5] Y.-L. Lee, J. Kleis, J. Rossmeisl, Y. Shao-Horn, D. Morgan, Prediction of solid oxide fuel cell cathode activity with first-principles descriptors. Energy & Environmental Science 4, 3966–3970 (2011).

[6] R. Jacobs, J. Hwang, Y. Shao-Horn, D. Morgan, Assessing Correlations of Perovskite Catalytic Performance with Electronic Structure Descriptors. Chemistry of Materials 31, 785–797 (2019).

[7] A. M. Deml, V. Stevanović, C. L. Muhich, C. B. Musgrave, R. O’Hayre, Oxide enthalpy of formation and band gap energy as accurate descriptors of oxygen vacancy formation energetics. Energy & Environmental Science 7, 1996–2004 (2014).

[8] R. B. Wexler, G. Sai Gautam, E. B. Stechel, E. A. Carter, Factors Governing Oxygen Vacancy Formation in Oxide Perovskites. Journal of the American Chemical Society 143, 13212–13227 (2021).

[9] A. Rothschild, W. Menesklou, H. L. Tuller, E. Ivers-Tiffée, Electronic Structure, Defect Chemistry, and Transport Properties of SrTi1-xFexO3-y Solid Solutions. Chemistry of Materials 18, 3651–3659 (2006).

[10] M. Vračar, A. Kuzmin, R. Merkle, J. Purans, E. A. Kotomin, J. Maier, O. Mathon, Jahn-Teller distortion around Fe4+ in Sr(FexTi1-x)O3-δ from x-ray absorption spectroscopy, x-ray diffraction, and vibrational spectroscopy. Physical Review B 76, 174107 (2007).

[11] J. Suntivich et al., Estimating Hybridization of Transition Metal and Oxygen States in Perovskites from O K-edge X-ray Absorption Spectroscopy. Journal of Physical Chemistry C 118, 1856–1863 (2014).

[12] F. Frati, M. O. J. Y. Hunault, F. M. F. de Groot, Oxygen K-edge X-ray Absorption Spectra. Chemical Reviews 120, 4056–4110 (2020).

[13] R. Muenstermann, T. Menke, R. Dittmann, R. Waser, Coexistence of Filamentary and Homogeneous Resistive Switching in Fe-Doped SrTiO3 Thin-Film Memristive Devices. Advanced Materials 22, 4819–4822 (2010).

[14] A. Sarantopoulos, R. Waser, R. Dittmann, Eightwise Switching Mechanism in Memristive SrTiO3 Devices and Its Implications on the Device Performance. Physica Status Solidi A 221, 2300483 (2024).

[15] M. Janousch, G. I. Meijer, U. Staub, B. Delley, S. F. Karg, B. P. Andreasson, Role of Oxygen Vacancies in Cr-Doped SrTiO3 for Resistance-Change Memory. Advanced Materials 19, 2232–2235 (2007).

[16] C. Baeumer et al., Spectromicroscopic insights for rational design of redox-based memristive devices. Nature Communications 6, 8610 (2015).

[17] C. Baeumer et al., Quantifying redox-induced Schottky barrier variations in memristive devices via in operando spectromicroscopy with graphene electrodes. Nature Communications 7, 12398 (2016).

[18] C. Baeumer et al., Subfilamentary Networks Cause Cycle-to-Cycle Variability in Memristive Devices. ACS Nano 11, 6921–6929 (2017).

[19] T. Heisig, C. Baeumer, U. N. Gries et al., Oxygen Exchange Processes between Oxide Memristive Devices and Water Molecules. Advanced Materials 30, 1800957 (2018).

[20] E. Sediva, W. J. Bowman, J. C. Gonzalez-Rosillo, J. L. M. Rupp, Investigation of the Eightwise Switching Mechanism and Its Suppression in SrTiO3 Modulated by Humidity and Interchanged Top and Bottom Platinum and LaNiO3 Electrode Contacts. Advanced Electronic Materials 5, 1800566 (2019).

[21] E. Mikheev, B. D. Hoskins, D. B. Strukov, S. Stemmer, Resistive switching and its suppression in Pt/Nb:SrTiO3 junctions. Nature Communications 5, 3990 (2014).

[22] K.-H. Son, H.-S. Lee, Grain boundary effect on the resistive switching characteristics of SrTi1-xFexO3 directly patterned via photochemical organic-metal deposition. Applied Surface Science 575, 151754 (2022).

[23] S. Asanuma, H. Akoh, H. Yamada, A. Sawa, Relationship between resistive switching characteristics and band diagrams of Ti/Pr1-xCaxMnO3 junctions. Physical Review B 80, 235113 (2009).

[24] A. Herpers, C. Lenser, C. Park, F. Offi, F. Borgatti, G. Panaccione, S. Menzel, R. Waser, R. Dittmann, Spectroscopic proof of the correlation between redox-state and charge-carrier transport at the interface of resistively switching Ti/PCMO devices. Advanced Materials 26, 2730–2735 (2014).

[25] W. C. Chueh, C. Falter, M. Abbott, D. Scipio, P. Furler, S. M. Haile, A. Steinfeld, High-Flux Solar-Driven Thermochemical Dissociation of CO2 and H2O Using Nonstoichiometric Ceria. Science 330, 1797–1801 (2010).

[26] D. N. Mueller, M. L. Machala, H. Bluhm, W. C. Chueh, Redox activity of surface oxygen anions in oxygen-deficient perovskite oxides during electrochemical reactions. Nature Communications 6, 6097 (2015).

[27] C. Baeumer, J. Li, Q. Lu et al. (with W. C. Chueh), Tuning electrochemically driven surface transformation in atomically flat LaNiO3 thin films for enhanced water electrolysis. Nature Materials 20, 674–682 (2021).

[28] M. Wuttig et al., Revisiting the Nature of Chemical Bonding in Chalcogenides to Explain and Design their Properties. Advanced Materials 35, 2208485 (2023).

[29] A. Sarantopoulos, K. Lange, F. Rivadulla, S. Menzel, R. Dittmann, Resistive Switching Acceleration Induced by Thermal Confinement. Advanced Electronic Materials 11, 2400555 (2025).

[30] M. Mladenović, M. Kaniselvan, C. Weilenmann, A. Emboras, M. Luisier, Termination-Dependent Resistive Switching in SrTiO3 Valence Change Memory Cells. ACS Applied Electronic Materials 7, 2839–2847 (2025).

[31] K.-J. Lee, C.-H. Wu, C.-J. Lee, D.-W. Chou, N.-F. Wang, Y.-H. Wang, Reset-Voltage Controlled Resistance-State and Applications of Forming-Free Fe-Doped SrTiO3 Thin-Film Memristor. Materials 17, 5021 (2024).

[E1] M. Buczek et al., Amorphous, Highly Conductive Pr0.7Ca0.3MnO3 for Area-Dependent Resistive Switching Devices. Advanced Electronic Materials (2026, accepted).

[E2] M. Buczek, Z. Moos, A. Gutsche, S. Menzel, R. Dittmann, Pr1-xCaxMnO3-Based Memristive Heterostructures: Basic Mechanisms and Applications. Chemical Reviews 125, 6156–6202 (2025).

[E3] M. Buczek et al., Large Area Pulsed Laser Deposition of Memristive Pr0.7Ca0.3MnO3 Heterostructures for Neuromorphic Computing. Thin Solid Films (2024).

# Checklist of Further Application Documents (AvH online portal)

| Document | Status / note |
| --- | --- |
| Curriculum vitae (max. 2 pages) | Condense from CV_Max_Buczek; focus: doctorate, methodological profile, publications, supervision |
| Research proposal (max. 5 pages) | This exposé – coordinate with Prof. Chueh before submission (AvH requirement: independently developed, coordinated with the host) |
| Complete list of publications | Incl. conference contributions and patent application |
| 1–3 key publications with justification | Recommendation: Chem. Rev. 2025 (command of the field, first author), Adv. Electron. Mater. 2026 (device innovation), Thin Solid Films 2024 (PLD methodology) |
| Doctoral certificate / proof | If applying before completion: declaration that the dissertation will be submitted within 6 months |
| Host’s statement + confirmation of research place (incl. mentoring agreement and co-funding commitment) | Prof. Chueh uploads directly to the AvH portal; raise the host contribution (approx. 1/3 of the fellowship; USA is a contributing country) early |
| Two expert reviews | Recommendation: Prof. R. Dittmann (doctoral supervisor) + one external, preferably international referee [e.g. from the NeuroSys consortium or the E-MRS environment] |

## Fellowship benefits (for orientation, as of 2026)

Base fellowship € 2,187.50/month (minus host contribution) + foreign allowance USA (€ 1,892 single or € 2,528–2,807 with family) + research cost allowance € 312.50/month + travel lump sums; family benefits (partner allowance € 205, child allowance € 400/100); afterwards optionally the Feodor Lynen Return Fellowship (up to 12 months, € 3,600/month) to bridge until group funding. Applications accepted at any time; selection meetings February/June/October; success rate approx. 40 %.